[image: image1.png]BURCHARTHs

farve&lakiabrikas
PRODUCT DESCRIPTION
TYPE: Aqua Air Single-Layer Topcoat |
APPLICATION: Aqua Air single Tayer topcoat can be used on metal and plastic. !
PROPERTIES: Produced on the basis of alkyd / acrylic with pigments free |
from hcavy metal, Containing corrosionpigment.

TECHNICAL DA’ - |
Density 1,05-1.40

Solids volume % 3644

Solids weight % 42-48
|pH 8,0:9,0

Theoretical coverage At40 pm 10 m? / Itr.

Recommended layer

Thickness 40 um dry-film, 100 m wet-film

Gloss Half-matt

For dilution
For cleaning

Safety and environment
Mixing ratio, weight

Demineralized water
Water / Butylglycol (9:1)
Se safety data sheet

Hardener -

Potife -

Shelf life 6 months from date of purchase

Storage Min. + 5°C, max. + 25°C

DRYING:

o Air drying at 20°C and 60% relative humidity: B
Layer thickness Dust dry | To handle
AL40 pm 12 hours | 24 hours

Recoatable: Min. 3 hours —max. 7 days.

Oven-drying or forced drying:

Deaeration

Stoving time Temperature

10 min,

20 min. 60-100°C

. |

Prodct deserption - Aqua Alr Single- ayer

Topeost- BFL AFS evised 25.10.05






[image: image2.png]|
PRE-TREATMENT:

The material must be clean and dry. No grease, oil, corrosion or iron scales.

COLD-ROLLED STEEL Degreasing and phosphating
HOT-ROLLED STEEL Shot blasting to SA 2% IS0 850111988
GALVANIZED STEEL Ask the technical service dept.
OTHER SURFACES RTe— dept.
| RECOMMENDED PRIMER ‘A;u'a Air Primer
APPLICATION:

The paint can be applied using the most known application techniques. If necessary contact
technical service.

Method Equipment | Visc. DIN 420°C
Spraying Afrmix 60-80 sec.
Airless 60-80 sec.
Airspraying | 60sec. | |

APPLICATION CONDITIONS:

The paint must be applied immediately after pre-treatment. During application — air tempera-
ture, paint temperature and material temperature must be above +15°C. Relative humidity
below 60%.

COMMENTS:

Available in RAL or NCS colours or any colour at your request. Ventilation during drying is
necessary.

The technical specifications are based on laboratory tests and can be used as instructive for the choice of pro-
ducts and working method. As we have no control of the users working conditions, we can only be responsible
Jfor the qualiy of the product. We thercfore recommend testing in own fuciltis 1o mieet the relevan demands

Prodct deserption- Aqua A Stgle-Layer Topeoat - BFL A'Srevised 25,1005




